Table 50.1. Wax-resin recipes used in experiments.

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| **Sample** | **Wax** | **Quantity (part)** | **Resin** | **Quantity (part)** | **Other** | **Quantity (part)** | |
| **A** | Unbleached beeswax | 7 | Dammar resin | 2 | Microcrystalline wax | 1 | |
| **B** | Unbleached beeswax | 7 | Dammar resin | 4 | Microcrystalline wax | 1 | |
| **C** | Unbleached beeswax | 7 | Dammar resin | 2 | Gum elemi | 1 | |
| **D** | Unbleached beeswax | 7 | Dammar resin | 2 | Colophony | 1 | |
| **E** | Unbleached beeswax | 7 | Dammar resin | 2 | Canada balsam | 1 | |
| **F** | Unbleached beeswax | all | — | — | — | | — |